## Slide 1: The CPM 401 cathodic protection diagnostic technology
Dr. Zoltan Lukacs
Indexon Ltd. P.
www.indexon.hu

## Slide 2: Diagnostic methods of cathodic protection
Conventional diagnostic procedures
  CP station survey
  Test point potential survey
  DCVG survey
  CIPS survey

## Slide 3: Evaluation of conventional diagnostic methods
The applicability of these methods is very limited under the following conditions:
  A great number of effective CP stations
  Interference
  Stray current
  Presence of effective sacrificial anode
  Dry or heavily polluted (oily) soil
Difficulties with integration of conventional methods in quality assurance systems.

## Slide 4: Limitations of conventional methods 1. A great number of CP stations
As the count of CP stations, that can be interrupted, is limited by the count of the available interrupters, the interrupted methods (Test point On/Off potential readings and CIPS measurements) provide distorted data in areas, where an excess number of effective CP stations are operating.

## Slide 5: Limitations of conventional methods 2. Interference
The conventional methods can verify the presence of interference only in those cases, when the interference is strong enough to be harmful to the affected structures.

## Slide 6: Limitations of conventional methods 3. Stray current
In the presence of stray current the conventional CP testing methods provide only approximate data, which is inadequate for correct evaluation.

## Slide 7: Limitations of conventional methods 4. Sacrificial anodes
In the presence of sacrificial anodes the conventional diagnostic methods can be applied very cumbersome (by interrupting each and every sacrificial anode). Furthermore, in cases where the sacrificial anodes are connected (welded) underground to the structure, the measurement data will be distorted similarly to the stray current case.

## Slide 8: Limitations of conventional methods 5. Dry or heavily polluted soil 1.
The precision of measurement can be strongly influenced by the high soil resistivity. In the conventional methods the measurement of soil resistance is not adequately solved apart from a few exceptions.

## Slide 9: Limitations of conventional methods 5. Dry or heavily polluted soil 2.
Erroneous measurement data in the chart of a conventional CIPS measurement.

## Slide 10: Limitations of conventional methods 6. Incompatibility with QA systems.
The conventional CP diagnostic technologies do not provide auxiliary data that could be used for qualifying the measurement (potential) data. Therefore, any attempt on the integration of these methods in modern quality assurance systems is restricted to formal acceptance criteria.

## Slide 11: Presentation of the CPM 401 technology
The technology is based on the following sources:
  Latest scientific results
  Requirement analysis
  Former development experiences

## Slide 12: Results of development 1.
Procedure for the determination of the contact resistance of the reference electrode
  The method can make the difference between the correct measurement (potential) data obtained at adequately low resistance points, and the distorted data measured at high resistance contacts. The distorted data are either corrected (if the error is sufficiently small) or discarded otherwise.

## Slide 13: Results of development 2.
Procedure for the determination of the IR free potential of a coating defect
  In the conventional measurement practice the measured OFF potential is generally identified with the IR-free potential. If current is flowing to the coating defect in this state for any reason then this assumption is false. A method was developed to assess the IR-free potential also in the cases when the nonzero current state cannot be achieved.

## Slide 14: Results of development 3.
  Alteration of measurement configuration
  In order to increase the measurement precision, the measurement configuration was altered with respect to the conventional CIPS measurements.

## Slide 15: Results of development 4.
Surface equipotential lines
Coating defect
Test point
Reference electrodes
Protected pipeline
CP station
Anode
Interrupter
Current flux lines
CIPS data logger
Conventional CIPS measurement configuration

## Slide 16: Results of development 5.
Modified CPM 401 CIPS measurement configuration
Surface equipotential lines
Coating defect
Test point
Reference electrode
Protected pipeline
CP station
Anode
Interrupter
Current flux lines
CPM 401 mobile data logger

## Slide 17: Results of development 6.
  A practice, suitable for quality assurance requirements, in the classification of measurement data includes:
  - Integrated data processing system
  - Automatic data qualifying algorithm
The Integrated data processing system
means that the data flow, from the measuring process down to the report, is designed in a way that no arbitrary human decision making or action, which could result in an erroneous assessment, is necessary either in data handling or in evaluation.

## Slide 18: Results of development 6.
The Automatic data qualifying algorithm
consist of two steps:
Separating the technically correct potential data from those, which were taken at a bad contact or high resistance point and are so much distorted, that they cannot be corrected, and should therefore be discarded.
Separating the useful data that bear technically relevant information on the level of cathodic protection.

## Slide 19: Components of the CPM 401 system
CPM 401 Data Logger
CPM 401 Expert program
CPM 401 Surveyor program
CPM 100 Interrupter
CPM CU2 Reference Electrode
CPM K1 Cable Backpack

## Slide 20: CPM 401 Data logger 1.
Four-channel AD-converter, range of -10 ... +10 V, resolution of 1.2 mV.
DA converter, range of -5 ... +5 V, output max. 0.25 A.
TTL Out channel, for driving an interrupter.
TTL In channel, for backpack distance signal counter.
GPS module for precise timing and location assessment.

## Slide 21: CPM 401 Data logger 2.
Battery operation, at least 12 hours of operation (if DA Out channel is inactive).
USB and RS232 communication channels for data transfer with master computers.
Data sampling frequency of max. 160 Hz, noise suppression optimized for the frequency range 50 .. 120 Hz, very stable analogous potential measurement input channels.

## Slide 22: CPM 401 Data logger 3.
Microprocessor operated, very flexibly programmable. Max. 32 averaged temporary storage addresses for each input channel.
128 MB built-in memory, capable of storing data of up to 24-hour long measurement series.
Simple measurement setup design and download by means of the CPM 401 Expert program.

## Slide 23: CPM 401 Data logger 4.
CPM 401 CIPS Data logger cabled for a DCPA measurement, the monitoring computer is laying on the data logger.

## Slide 24: CPM 401 Expert program
Desktop application for Windows XP operation system.
Clear, easily accessible user interface.
MS Access database connection.
Displaying all measurement and related data.
Communication with the CPM401 Data logger.
Communication with the Surveyor database.
Reporting, printing, saving in Excel format.
Exporting data in Excel-compatible text file.

## Slide 25: CPM 401 Surveyor program
Hand-held palmtop application for Win CE 4.2 operation system, PSION Workabout Pro computer.
Real- time displaying measurement and related (e.g. GPS) data, signal on receiving erroneous data.
Clear user interface, storage of land object data in database.
Easy data upload/download to/from the Expert program database.

## Slide 26: CPM 100 Interrupter
Max. 60 V nominal potential limit.
Max. 100 A nominal current limit.
The interrupter can be overloaded up to 150A for short time without damage.
Polarity protection.

## Slide 27: CPM CU2 Reference electrode
Special Cu/CuSO4 reference electrode designed specifically for the requirements of the CPM 401 technology.

## Slide 28: CPM K1 Cable backpack
The CPM K1 backpack is fully compatible with the popular GLOBAL type backpacks.

## Slide 29: Measurement methods of the CPM 401 technology 1. Conventional methods
CP station survey.
Test point potential survey.
General purpose potential monitoring.
Conventional DCVG survey.
Conventional CIPS survey.
Conventional CIPS survey with static data logger.
Soil resistivity measurement.

## Slide 30: CP Station survey
The Expert and Surveyor programs are capable of maintaining (entering, editing and commenting) data of land objects (e.g. CP stations, drainage points, anodes) and the related current and potential data.
The data are stored in MS Access database and can be easily retrieved for creating queries and reports.

## Slide 31: Test point survey
The data of test points and other land objects can be downloaded to the Surveyor program from the database of the Expert program. At these measurements the CPM4 401 Data logger works in Monitoring mode, like a multimeter. In this mode the data logger samples the signal at every 0.5 s. With appropriate timing (e.g. 4 s ON, 1 s OFF) the OFF potential value is always measured in the same phase of the OFF period, thus obtaining an OFF potential value much more reproducible, precise and comparable than a data obtained with a conventional multimeter. It is possible to measure the contact resistance of the reference electrode also in Monitoring mode thus enabling the Operator to exclude incorrect measurement data.

## Slide 32: Potential monitoring
General purpose potential monitoring, to measure Potential vs. Time data series, e.g. for stray current monitoring purposes. It is possible to carry out a four-channel measurement without reference electrode resistance compensation or a two-channel measurement with compensation.

## Slide 33: DCVG survey
The ‘Delta’ value of the conventional DCVG measurements is displayed both in analogous and numerical form. Data can be obtained only with application of the reference electrode resistance compensation.

## Slide 34: CIPS survey
In this measurement a single ‘Mobile’ data logger is operated. Data can be obtained only with application of the reference electrode resistance compensation. Due to the enhanced data qualifying algorithm, it is not necessary to hold at least one of the reference electrodes always on the ground, the two reference electrodes can be lifted and placed simultaneously, and thus a more effective way of measurement is implemented.

## Slide 35: CIPS survey with static data logger
Conventional CIPS measurement with an additional static data logger, located at the starting test point. The data of the mobile and the static loggers are coupled by the Expert program database.

## Slide 36: Soil resistance measurement
The equipment is capable of measuring soil resistance according to the Wenner- or the Schlumberger method. The obtained data are stored with the corresponding GPS-coordinates and are available as reports in Excel-compatible text file or as reports in Excel format.

## Slide 37: Measurement methods of the CPM 401 technology 2. New methods
DCPA (Direct Corrosion Potential Assessment)
DCPA-WL (DCPA-wireless)
XDCPA (DCPA wit external current source)
XDCPA-WL(XDCPA-wireless)
SAPT (Sacrificial Anode Performance Testing)
SCIT (Stray Current and Interference Testing)

## Slide 38: DCPA (Direct Corrosion Potential Assessment)
The method is the novelty of the CPM 401 technology. The measurement is carried out similarly to the CIPS measurement with a remote static data logger, but the evaluation of the data provides the additional value of the calculated IR-free potential in the vicinity of coating defects. After uploading data to the Expert program, it calculates the IR-free potential values obtained from both the close and the remote measurement data. In the presence of distorting effects the method provides the known most accurate approximation of the IR-free potential, thus enabling a more accurate determination of the level of protection also in the cases when the conventional CIPS methods do not give reliable data.

## Slide 39: Typical application fields of the DCPA method
There are a number of uninterrupted CP stations in the region of the measurement.
Significant stray current or corrosion macrocell activity prevails in the measurement area.
Non-interrupted sacrificial anodes are operated in the measurement area.

## Slide 40: Application scheme of DCPA 1.
Connection of CPM 401 Data logger in mobile logger application.
Surface equipotential lines
Coating defect
Test point
Reference electrode
Protected pipeline
Transformer-rectifier
Anode
Interrupter
Current flux
CPM 401 mobile data logger
CPM 401 static data logger for remote potential monitoring

## Slide 41: Application scheme of DCPA 2.
Execution of a DCPA measurement. The left side reference electrode is directly over the line.

## Slide 42: Application scheme of DCPA 3.
DCPA raw data, as a function of time, with a number of erroneous points.

## Slide 43: Application scheme of DCPA 4.
DCPA filtered and processed data, as a function of distance, with the calculated IR-free potentials at the coating defects.

## Slide 44: DCPA-WL (wireless) 1.
A modification of the DCPA method, where the cable between the test point and the mobile logger is not applied. A great advantage of the method is that it works also in those areas (communal regions, busy traffic, absence of test points, etc.), where the measurements with a cable between the mobile logger and the test point can be carried out only very cumbersome or cannot be carried out at all.

## Slide 45: DCPA-WL 2.
A further application field of the method is the regular maintenance surveys or the measurements after changing the current output somewhere in the system. With this method it is possible to determine the IR-free potential at critical points (e.g. large coating defects, interference suspect locations, minimum points between CP stations), even if no close cable connection is available due to the lack of nearby test points. Thus the consequences of any change in CP current settings can be checked very fast and accurately.

## Slide 46: Comparison of IR-free potential data obtained with DCPA and DCPA-WL
Comparison of IR-free potential data obtained with DCPA and DCPA-WL (wireless) methods, using the remote potential data.

## Slide 47: XDCPA
A modified version of the DCPA method, where the interruption of the CP stations is not required because reference signals of another type are used. The method is applicable on sites where no CP system is operated, or the applied CP system cannot be interrupted (e.g. because sacrificial anodes are used with no testing facilities).

## Slide 48: XDCPA-WL
A variation of the XDCPA method where – similarly to the DCPA-WL method – no cable reel is used between the mobile logger and the test point, and the remote potential of the structure is measured with a static data logger, located at the nearest pest point. The application fields are also similar to those of the DCPA-WL method, i.e. sites where the cable reel of the mobile logger cannot be used due to danger of accident or material losses.

## Slide 49: SAPT
The SAPT (Sacrificial Anode Performance Testing) method is used for determining the IR-free potentials of the sacrificial anode and the protected structure, also in those cases, when the anode and the protected structure cannot be disconnected (i.e. they are connected with underground welded cables).
In case of standalone anodes the method is capable of determining the current flowing between the anode and the structure. In case of continuous (e.g. ribbon) anodes the relative current intensity distribution can be determined.

## Slide 50: SCIT 1.
The SCIT (Stray Current and Interference Testing) method is designed to fight the stray currents and the interference, the two most dangerous phenomena in cathodic protection. The SCIT method is a complex procedure which can investigate the two phenomena in one step. The evaluation provides quantitative, numeric data for the characterization of cross-effects between interference-suspected current sources (e.g. CP stations) and stray current sources. Upon the evaluation of results, recommendations can be made on the optimal level of current outputs of the current sources and on other necessary actions in order to decrease interference and stray current danger.

## Slide 51: SCIT 2.
The resource requirement of the SCIT method is very high in complicated systems (it needs a great number of data loggers), and the evaluation of the data requires special mathematical knowledge. Therefore, this method is available exclusively as a service of the designer of the technology.